# Sincere              Open                 Win-Win

| # Liquid Silicone Rubber Technical Data Sheet Sanesil LSR8100 A/B SX0610-2023-27 V2 |  |
| --- | --- |
| Description: Sanesil LSR8100 A/B is a two-component general purpose liquid silicone rubber designed for producing high clarity, high tear strength parts through injection process after A/B mix with ratio of 1/1. |  |
| Special properties: Main applications: | - Excellent mold release and easily pigmented - Superior clarity - High performance physicals, high tear and elongation - Excellent rebound resilience - Soft, skin-like feel when molded - Baby care parts - Respiratory mask - Automotive applications: valves, gaskets, seals - Skin contact parts like liners - Balloons |

Mechanical properties

| Grade | A/B viscosity Pa.s | Appearance A/B | Density (g/ cm3) | Hardness (Shore A) | Tensile strength (MPa) | Elongation at break (%) | Tear strength (N/mm) |
| --- | --- | --- | --- | --- | --- | --- | --- |
| Test method | ISO 3219:1995 |  | ISO 2781:2018 (Method A) | ISO 7619- 1:2010 | ISO 37:2011 (Type 1) | ISO 37:2011 (Type 1) | GB/T 529-2008 (Method C) (MOD ISO 34- 1:2010 (Method C)) |
| LSR 8120 | 285/272 | Transparent/ transparent | 1.08 | 19 | 6.5 | 950 | 14 |
| LSR 8130 | 275/281 | Transparent/ transparent | 1.10 | 30 | 8.0 | 760 | 21 |
| LSR 8140 | 247/237 | Transparent/ transparent | 1.13 | 41 | 9.0 | 630 | 28 |
| LSR 8150 | 250/251 | Transparent/ transparent | 1.12 | 50 | 9.3 | 580 | 38 |
| LSR 8160 | 249/244 | Transparent/ transparent | 1.11 | 59 | 9.0 | 500 | 35 |

Sincere              Open                 Win-Win

Slabs 160mm*160mm*2mm at 177℃ cured for 5 minutes with hot mold. Compression set slabs at 177℃ cured for 10 minutes with cold mold. Compression set test condition:177℃*22hours, 25%. These data are approx.

Please note: The typical properties are not intended for use in preparing specifications for any particular applications. Please contact our Technical

Service Department for more detailed data.

Instruction of use ： Cure is dependent upon molding temperature and part size. The same lot part A and B components of Sanesil  LSR8100A/B  are  designed to  be  mixed  in  equal  parts  using  standard  liquid  injection molding processing equipment and techniques with the mixing temperature lower than 35°C. Airless mixing, metering and dispensing equipment are recommended for production operations. Accurate measuring and complete mixing are essential factors in obtaining consistent results.

Cleaning ：Special care must be taken to assure clean moulds and a clean work area with no organic rubbers used on the same processing equipment. Traces of foreign materials can poison the catalyst and inhibit the cure. All metering and mixing equipment should be thoroughly cleaned. Polymer systems, which contain traces of amines, sulfur, nitrogen oxide, organotin compounds and carbon monoxide can interfere with the cure of this product and should be avoided.

Packaging：Sanesil LSR8100A/B is available in 20 kg pails or 200 kg drums.

Sincere              Open                 Win-Win

Storage and shelf life:

This series may be stored in the original, unopened container at a temperature between 0°C and 30°C, can be     stored for 12 months from the date of manufacturing. Beyond this date, we no longer guarantees that the product meets the sales specifications.

For More Product Information, Please Visit Our Website: www.sanezen.com

Contact: Plant Address: Baishou Road, North District of Xuan Zhou Economic Development Zone, Xuan Cheng City Anhui Province, China. Commercial Address: Room 1606- 1608, Boda Commercial Buildings, No. 11 Puhuitang Road Xuhui District, Shanghai, China 200030 Tel: +86 21 6487 9251 Fax: +86 21 5106 2693 E-mail: kevenwang@sanezen.com

Warning to the users: The information contained in this document is given in good faith based on our current knowledge. It is only an indication and is in no way binding, particularly as regards infringement of or prejudice to third party rights through the use of our products. Sanezen guarantees that its products comply with its sales specifications. This information must on no account be used as a substitute for necessary prior tests which alone can ensure that a product is suitable for given use. Determination of the suitability of product for the uses and applications contemplated by users and others shall be the sole responsibility of users. Users are responsible for ensuring compliance with local legislation and for obtaining the necessary certifications and authorisations. Users are requested to check that they are in possession of the latest version of this document and Sanezen is at their disposal to supply any additional information.